## Slide 1
Valve design challenges in renewable HVO severe service
CONFERENCE
ORGANIZERS

## Slide 2: Valve design challenges in renewable HVO severe service
Mr. Mikko Vuolanto | Senior Specialist, Valves and Materials Engineering

## Slide 3: Outline
Last 20 years of renewable fuels business have seen a raising interest of hydrogen treated renewable fuels deriving from multiple feedstocks.
This presentation summarizes some experiences related to valves in such production facilities.
Notes: Framework
Personally, I have been working with valves in these processes for more than 15 years
Now involved on my 9th major greenfield project
Projects are heavily protected by IPR rights of licensors and therefore, this presentation mostly reflects the general knowledge

## Slide 4: Contents
Briefly of severe service
Challenges of HVO processes
Mitigation strategies & practical experience
Briefly about the future
Summary

## Slide 5: Briefly on severe service

## Slide 6
In this presentation, severe service is to be understood as a service where standard or commodity valves will not succeed, even when valves themselves are executed with highest quality standards

## Slide 7: Challenges of HVO processes

## Slide 8: Process challenges, general
Challenging materials selection compared to trad. hydrotreating
Process feedstock changes can be critical
Chemistry differs from mineral based feedstocks
Typically include
  Clean circulation
    Solution by process engineering
  Non-clean circulation
    Solution by materials engineering
→ Somewhere in between the segregation is done with valves

## Slide 9: Process challenges, PTU/HTU
High Acid number
Impurities still in the flow media
Can typically be handled through materials engineering
Apart from that, valves typically mostly of standard design

## Slide 10: Process challenges, hydrotreat
  High pressure, high temperature
  Chlorine
  Acid formation
  CO and CO2
  Catalyst remains
  Alternating conditions (TA - parallel equipment - etc)
  Role of feed through earlier units
Critical issues outside normal operation
Highly dependent of feed
Normal operation conditions are above product autoignition temperature, no room for failures
Redundancy requirements in terms of possible corrosion

## Slide 11: Valve challenges, hydrotreat
  Correct coating selection
  Resistance to catalyst remains
  Chlorine resistance
    SCC
  Acidic service
    SCC
    Other corrosion types
Many applications require detailed valve design considerations
  Cavity free designs
  Resistance to alternating conditions
  Bearing design

## Slide 12: Practical experience

## Slide 13: Key practical experience
Material grade selection issues
Ball valve coating corrosion resistance to match body material
  Std CrC can be problematic
  Shift to SF coatings
Alternating conditions are difficult to tackle
EN ISO 15848-1 AH foreseen
  Coke forming capability of renewable feedstocks is less
  Several streams above auto ignition temperature
In particular for ball valves, not all designs are acceptable
Valve coatings running torque

## Slide 14: Mitigation strategies

## Slide 15: Mitigation strategies
Equipment failures in these processes typically are due to corrosion. This can be mitigated in several ways
  Materials engineering
  Process engineering
  Equipment design
Typically, multiple reasons, acting simultaneously
  Holistic view is the key to success
Focus on long term solutions, integrated with best HSE practices

## Slide 16: Mitigation strategies, process engineering
Mitigating limiting factors by more detailed engineering
  Flushing
  Heat tracing
  Additional equipment
Integrated design engineering by multiple engineering disciplines (”pipeline” model is more vulnerable)

## Slide 17: Mitigation strategies, Materials engineering
Use of higher alloys, even above Ni-alloys
Use of lower alloys, general corrosion is predictable
Possibilities outside metallic materials
For active selection, the following is a must
  Deep understanding of corrosion mechanisms in the process, relevant to the current feedstock;
  Deep understanding and co-engineering with manufacturers

## Slide 18: Mitigation strategies, Valve design
Many times, simple product with less parts & well engineered offers good performance
Understand that there are no general solutions in severe service
Some realised designs in HVO severe service
  Cavity free design
  Metallurgical bonding for coatings
  Efficient FE design to EN 15848-1 AH class
  Unidirectional designs
  Optimised spring assistance

## Slide 19: Future

## Slide 20: About the future
Feedstock development
  Feedstocks to be more diverse and dirtier as only waste is accepted as a feedstock
Role of process design
  Understanding the small details define success or failure
Valve design development
  Even better corrosion resistance for coatings
  Erosion/corrosion mitigation by valve engineering
  Compliance to latest FE, typetesting, severe service standards

## Slide 21: Summary

## Slide 22: Wrap-up
Valve solutions for renewable HVO severe service are not yet established. Many details still not solved
Valves play critical role especially in safety functions, no room for malfunction
Many valve solutions are adaptations from mineral oil based processes. Actual suitability is a question

## Slide 23
Thank You ! Any questions ... ?
Contacts
Mr. Mikko Vuolanto
Email mikko@vuoplan.fi
Tel +358407397978

## Slide 24
ORGANIZING SECRETARIAT
Ph. +39 035 3230904
e-mail info@industrialvalvesummit.com
www.industrialvalvesummit.com
CONFERENCE ORGANIZERS
Ph. +39 3474908420
e-mail segreteria@valvecampus.com
www.valvecampus.com
Thanks